## Slide 1
X. Low energy electron diffraction (LEED)
10-1. 2-dimensional surface structures
Bulk: 14 Bravais lattices
Surface: 5 surface lattices
----- describe all possible periodic
surface structures
----- Miller index
----- structure = lattice point + basis
----- derivation by symmetry

## Slide 2
(a) Rectangular lattice (a  b,  = 90o)
(b) Centered rectangular lattice (a  b,  = 90o)

## Slide 3
(c) Parallelogram (oblique) lattice (a  b,   90o)
(d) square lattice (a = b,  = 90o)

## Slide 4
(e) Hexagonal lattice (a = b,  = 120o)
We have shown that there are only five plane
lattices in Chapter 3-1.
Example:
The ideal Si(111) surface: a hexagonal lattice.
The ideal Si(100) surface: a square lattice.
The (110) surface of Au: a rectangular lattice.
FCC

## Slide 5
10-2. Techniques for surface structure
determination
LEED (Low energy electron diffraction)
RHEED (Reflection high energy electron
diffraction)
STM (Scanning tunneling microscope)
SEXAFS (Surface extended X-ray
absorption fine structure)
In this course, LEED and RHEED will be
covered.

## Slide 6
4-grids LEED optics

## Slide 7
http://www.omicron.de/cache/media_GB_IMG_0093C_freigestellt%5B2467%5D_20111208-122653_omicronmedia_image_paddedthumbnailscheme_ffffff_800x1200.jpg

## Slide 8
Electron escape depth and surface sensitivity
http://www.globalsino.com/micro/TEM/images/TEM9923.gif

## Slide 9
The reciprocal lattice of the surface in LEED
Total scattering amplitude F for LEED is
: the electron density in the volume that
electrons are scattered and collected in the
detector (screen).

## Slide 10
In LEED, electrons are diffracted from volume within electron escape depth. If the electron beam size is 100 nm and the escape depth is 0.5 nm, the volume is in a disk shape.

## Slide 11
10-3. Ewald sphere construction the Si(100)
ideal surface in LEED
The atomic structure of the Si(100) ideal
surface
110
-110

## Slide 12
Ewald sphere construction and the expected LEED pattern

## Slide 13
However, the LEED pattern of as-cleaned Si(100) is not a square lattice
The LEED pattern for the Si(100) surface cleaned at 950 is double domain Si(100)-2x1 shown below, rather than Si(100)1x1

## Slide 14
http://upload.wikimedia.org/wikipedia/en/thumb/c/c4/Si100Reconstructed.png/639px-Si100Reconstructed.png
Explain this pattern later!

## Slide 15
> LEED using different electron kinetic energies
kinetic energy of electron increases 
k  radius of Ewald sphere 
 diffracted spots move inwards the sreeen
10
10
2B
< 2B

## Slide 16
Low E
High E

## Slide 17
III. Surface reconstruction (defined in the real
space)
Wood’s notation
(a) For a reconstructed surface
Where M is the chemical element, (hkl) is the plane, R is the rotation  angle between the axes of surface and bulk

## Slide 18
For example: Si(100)2x1
LEED pattern of single domain Si(100)2x1

## Slide 19
http://www.chem.qmul.ac.uk/surfaces/scc/scat1_6a.htm

## Slide 20
Another domain
Supposition of two domain 
double domain of Si(100)2x1

## Slide 21
Si(111) surface reconstructions and their LEED patterns
What are the reciprocal lattices of the Si(111)1x1, Si(111)2x1, and Si(111)7x7 surfaces?
What are the LEED patterns of the Si(111)1x1, Si(111)2x1, and Si(111)7x7 surfaces?
Question

## Slide 22
http://www.fhi-berlin.mpg.de/KHsoftware/Balsac/BalsacPictures/SSDfig99.gif
Picture from the NIST Surface Structure Database
Si(111)1x1

## Slide 23
http://www.fhi-berlin.mpg.de/KHsoftware/Balsac/BalsacPictures/SSDfig89.gif
Si(111)2x1

## Slide 24
http://www.fhi-berlin.mpg.de/KHsoftware/Balsac/BalsacPictures/SSDfig91.gif
Si(111)7x7

## Slide 25
http://www.geocities.jp/mitoh6/das7x701.jpg

## Slide 26
http://www.desy.de/~hasunihh/poster/beug/img1.jpg

## Slide 27
Practice for wood’s notation:
http://www.chem.qmul.ac.uk/surfaces/scc/scat6_4.htm
http://www.chem.qmul.ac.uk/surfaces/scc/scat6_1.htm

## Slide 28
100
1x2

## Slide 29
100
110
2x2
2x2

## Slide 30
100
110
c2x2
c2x2

## Slide 31
Substrate:
fcc (111)
Substrate unit cell
Surface or abrorbate unit cell
2x2

## Slide 32
Substrate:
fcc (111)

## Slide 33
10-5. Adsorbate surface structure
For an adsorbate surface
Where M is the chemical element, (hkl) is the plane, R is the rotation  angle between the axes of surface and bulk, and A is the adsorbate.

## Slide 34
Example #1 Ni(110)-C2x2-O

## Slide 35
Example #2 Coadsorption
2x2