## Slide 1
XII. Electron diffraction in TEM
JEOL
JEM-ARM200FTH
Spherical-aberration Corrected Field Emission Transmission Electron Microscope
Newest TEM in MSE

## Slide 2
Other TEM in MSE
JEOL JEM-3000F
JEOL JEM-2100

## Slide 3
Diffraction pattern: scattered in the same direction; containing information on the angular scattering distribution of the electrons
Image plane (bottom)
Simple sketch of the beam path of the electrons in a TEM
The diffraction pattern and the image are related through a Fourier transform.

## Slide 4
12-1. Electron radiation
(i) ~ hundreds Kev
Typical TEM voltage: 100 – 400 KV
Relativistic effect should be taken into account!
SEM typically operated at a potential of 10 KV  v ~ 20% c (speed of light)
TEM operated at 200 kV  v ~ 70% c.
highly monochromatic than X-ray

## Slide 5
Massless particle:

## Slide 6
h = 6.62606957×10-34 m2kg/s
m0 = 9.1093829110-31 Kg
c = 299792458 m/s
e = 1.60217657×10-19 coulombs
1eV = 1.60217656510-19 J (Kgm2/s2)

## Slide 7
For 200 KV electrons

## Slide 8
For 20 KV electrons

## Slide 9
For X-ray
Wavelength = 1.542 Å
J

## Slide 10
(ii) electrons can be focused
c.f. x-ray is hard to focus
(iii) easily scattered
: form factor for electron and
x-ray, respectively
Form factor for electron includes nucleus
scattering!
(iv) need thin crystals
＜1000Å, beam size  m

## Slide 11
12-2. Bragg angle is small
for 100 KeV
Assume d = 2Å
for 200Kev

## Slide 12
  12-3. d spacing determination is not good
(brevity)
For fixed 
we can get more accurate d at higher angle!
In TEM
Not good for d determination!

## Slide 13
12-4. Electron diffraction pattern from a single
crystalline material
Example: epitaxial PtSi/p-Si(100)
Ewald sphere construction:
 is very small k is very large compared to the lattice spacing in the reciprocal space

## Slide 14
(1) An electron beam is usually incident along the zone axis of the electron diffraction pattern.

## Slide 15
The sample can be tuned along another zone axis [xyz] . All the spots in the diffraction pattern belongs the zone axis [xyz].

## Slide 16
12-5. Electron diffraction pattern from a
polycrystalline material
Example: polycrystalline PtSi/p-Si(100)

## Slide 17
Ewald sphere constructions for powders and polycrystalline materials

## Slide 18
12-6. diffraction and image (bright field, dark field)
(a) Bright field image
http://labs.mete.metu.edu.tr/tem/TEMtext/TEMtext.html

## Slide 19
(b) Dark filed image
http://labs.mete.metu.edu.tr/tem/TEMtext/TEMtext.html

## Slide 20
http://www.microscopy.ethz.ch/BFDF-TEM.htm
Example: microcrystalline ZrO2
Diffraction
pattern
Bright-Field
Image
Dark-Field
Image
BF image: some crystals appear with dark contrast since they are oriented (almost) parallel to a zone axis (Bragg contrast).
DF image: some of the microcrystals appear with bright contrast, namely such whose diffracted beams partly pass the objective aperture.