## Slide 1
3-1 Symmetry elements
III Crystal Symmetry
(1) Translation:
Example: 1D lattice:
2D lattice:
3D lattice:
Crystal = “motif” repeated at each lattice point
Atom, molecule

## Slide 2
(2) Rotation symmetry
one fold 1
two fold (diad ) 2
three fold (triad ) 3
Four fold (tetrad ) 4
Six fold (hexad ) 6

## Slide 3
Proof: There are only 1, 2, 3, 4, and 6 fold
rotation symmetries for crystal with
translational symmetry.
The space cannot
be filled!
graphically

## Slide 4
Axis A, angle 
n: integer
n fold axis
Notation n
Example:
A
4
Only certain types of rotations are consistent with lattice
Periodicity (kepler):
p: integer:

## Slide 5
p | cos |  | n
3 | -1 | 180o | 2
2 | -1/2 | 120o | 3
1 | 0 | 90o | 4
0 | 1/2 | 60o | 6
-1 | 1 | 0o | 1
Crystallographic
rotation axes

## Slide 6
mirror
RH
LH
LH
RH
(3) Reflection (mirror) symmetry m
(4) Inversion symmetry (center of symmetry)
Examples:
C = C
Cl
Cl
H
H
m
Example:
C = C
Cl
Cl
H
H
i

## Slide 7
Enantiomorphism
Enantiomorphic bodies have a “handedness” (chirality)
e.g. your left and right hand
They can not be made to coincide by translation or rotation,
only by reflection (your hand) or inversion
Example
C
H
X
F
Cl
C
H
X
F
Cl
Note: a body with reflection or inversion symmetry can not
be chiral.

## Slide 8
= Rotate by
，then invert.
(a) one fold rotation inversion (
(b) two fold rotation inversion (
= mirror symmetry (m)
(5) Rotation-Inversion axis
Combinations of
Symmetry Elements
Side view
i
A
top view
i
m
A

## Slide 9
(c) inversion triad ()
3
= Octahedral site in
an octahedron

## Slide 10
(d) inversion tetrad ()
= tetrahedral site in a
tetrahedron
x
(e) inversion hexad ()
Hexagonal close-packed (hcp) lattice
x

## Slide 11
(6) Screw axis: rotation about A, then translation by
 // A
31
A
32
A
t: lattice translation
vector along A
In a lattice: translation vector along A is t
requirement:

pitch
for the "crystallographic"
screw axes

## Slide 12
41
42
43
4
21
2
31
32
3

## Slide 13
61
62
63
64
65
6

## Slide 14
Example of 63 screw axis: hcp
A
B
Basal
plane
63

## Slide 15
(7) Glide plane: translation by  (in m), reflect about m
In lattice: t = translation distance along glide direction
Example: diamond cubic
Glide plane
Glide direction

## Slide 16
Screw axis and glide plane involve translation: symmetry elements for space group not for point group!
Symmorphic space group is defined as a space group that may be specified entirely by symmetry operation acting at a common point (the operations need not involve τ) as well as the unit cell translation. (73 space groups)
Nonsymmorphic space group is defined as a space group involving at least a translation τ.

## Slide 17
3-2-1. 1-D lattice
3 types of symmetry can be arranged in a 1-D lattice
mirror symmetry (m)
= 2-fold rotation (2)
= center of symmetry ()
3-2. Fourteen Bravais lattice structures

## Slide 18
Two ways to repeat 1-D  2D
(1) maintain 1-D symmetry
(2) destroy 1-D symmetry
3-2-2. 2-D lattice
m 2

## Slide 19
(a) Rectangular lattice (; 90o)
Maintain mirror symmetry m
(; 90o)

## Slide 20
(b) Center Rectangular lattice (; 90o)
Maintain mirror symmetry m
(; 90o)
Rhombus cell
(Primitive unit cell)
; 90o

## Slide 21
(c) Parallelogram lattice (; 90o)
Destroy mirror symmetry

## Slide 22
(d) Square lattice (; 90o)
a
b
(e) hexagonal lattice (; 120o)

## Slide 23
Symmetry elements in 2D lattice
Rectangular = center rectangular?

## Slide 24
3-2-3. 3-D lattice: 7 systems, 14 Bravais lattices
Starting from parallelogram lattice
(; 90o)
(1)Triclinic system 1-fold rotation (1)
b



a
c
(; 90o)

## Slide 25
lattice center symmetry at lattice point as shown above which the molecule is isotropic ()

## Slide 26
one diad axis
(only one axis perpendicular to the drawing plane maintain 2-fold symmetry in a parallelogram lattice)
(2) Monoclinic system
(; )

## Slide 27
(1) Primitive monoclinic lattice (P cell)
a
b
c
(2) Base centered monoclinic lattice
c
b
a
B-face centered monoclinic lattice

## Slide 28
The second layer coincident to the middle of
the first layer and maintain 2-fold symmetry
Note: other ways to maintain 2-fold symmetry
a
c
b
A-face centered
monoclinic lattice
If relabeling lattice coordination
A-face centered monoclinic = B-face centered

## Slide 29
(2) Body centered monoclinic lattice
Body centered monoclinic = Base centered monoclinic

## Slide 30
So monoclinic has two types
1. Primitive monoclinic
2. Base centered monoclinic

## Slide 31
(3) Orthorhombic system
a
b
c
(; )
3 -diad axes

## Slide 32
(1) Derived from rectangular lattice
(; 90o)
 to maintain 2 fold symmetry
The second layer superposes directly on the first layer
(a) Primitive orthorhombic lattice
a
b
c

## Slide 33
(b) B- face centered orthorhombic
= A -face centered orthorhombic
c
a
b
(c) Body-centered orthorhombic (I- cell)

## Slide 34
rectangular
body-centered orthorhombic
 based centered orthorhombic

## Slide 35
(2) Derived from centered rectangular lattice
(; 90o)
(a) C-face centered Orthorhombic
a
b
c
C- face centered orthorhombic
= B- face centered orthorhombic

## Slide 36
(b) Face-centered Orthorhombic (F-cell)
Up & Down
Left & Right
Front & Back

## Slide 37
Orthorhombic has 4 types
1. Primitive orthorhombic
2. Base centered orthorhombic
3. Body centered orthorhombic
4. Face centered orthorhombic

## Slide 38
(4) Tetragonal system
a
b
c
(;
)
One tetrad axis
starting from square lattice
(; )

## Slide 39
starting from square lattice
(; )
(1) maintain 4-fold symmetry
(a) Primitive tetragonal lattice
First layer
Second layer

## Slide 40
(b) Body-centered tetragonal lattice
First layer
Second layer
Tetragonal has 2 types
1. Primitive tetragonal
2. Body centered tetragonal

## Slide 41
(5) Hexagonal system
a = b  c;
 =  = 90o;  = 120o
b
a
c



One hexad axis
starting from hexagonal lattice (2D)
a = b;  = 120o

## Slide 42
(1) maintain 6-fold symmetry
Primitive hexagonal lattice
b
a
c



(2) maintain 3-fold symmetry
a
b
c



1/3
2/3
1/3
2/3
a = b = c;
 =  =   90o

## Slide 43
Hexagonal has 1 types
1. Primitive hexagonal
Rhombohedral (trigonal)
2. Primitive rhombohedral (trigonal)

## Slide 44
(6) Cubic system
4 triad axes ( triad axis = cube diagonal )
Cubic is a special form of Rhombohedral lattice
Cubic system has 4 triad axes mutually inclined along cube diagonal
b
a
c



a = b = c;
 =  =  = 90o

## Slide 45
(a) Primitive cubic
 = 90o
b
a
c



a = b = c;
 =  =  = 90o
(b) Face centered cubic
 = 60o
a = b = c;
 =  =  = 60o

## Slide 46
(c) body centered cubic
 = 109o
a = b = c;
 =  =  = 109o

## Slide 47
cubic (isometric)
Primitive (P)
Body centered (I)
Face centered (F)
Base center (C)
Special case of orthorhombic with a = b = c
a = b  c
Tetragonal (P)
Tetragonal (I)?
Cubic has 3 types
1. Primitive cubic (simple cubic)
2. Body centered cubic (BCC)
3. Face centered cubic (FCC)
3 fold rotation
disappears

## Slide 48
http://www.theory.nipne.ro/~dragos/Solid/Bravais_table.jpg
= P
= I
= T P
