## Slide 1
IX. X-ray diffraction
9-1. Production of X-ray
http://www.arpansa.gov.au/radiationprotection/basics/xrays.cfm
Vacuum, thermionic emission, high voltage,
and a target

## Slide 2
Braking radiation
Characteristic
X-ray
Auger electrons
Energetic electron hitting a target

## Slide 3
Target
v0
v1
v2
(i) Braking radiation:
I

V1
V2
V2 > V1
Short wavelength limits

## Slide 4
Excitation
source
K
L1
L2
L3
K
L1
L2
L3
Characteristics
X-Ray photon
k
L1
L2
L3
Auger
electron
Radiative
transition
Nonradiative
transition
M
}
{
K
K2
K1
1S
2S
2P
3S
The figure in Note is wrong!
(ii) characteristic radiation

## Slide 5
a typical X-ray spectrum

## Slide 6
(iii) Cu K radiation
Cu K1 =1.54050 Å
Cu K2 =1.54434 Å
Cu K =1.5418 Å
High angle line
Low angle line
Why we can resolve K1 and K2 double
lines at high angle?

## Slide 7
9-2. X-ray diffraction
(i) Laue method:  variable, white
radiation,  fixed
(ii) Diffractometer method:  fixed,
characteristic radiation,  variable
(iii) Powder method:  fixed, characteristic
radiation,  variable
(iv) Rotating crystal method:  fixed,
characteristic radiation,  variable

## Slide 8
9-2-1. Laue method

## Slide 10
(1) Laue condition
Von Laue derived the “ Laue conditions “ in
1912 to express the necessary conditions for
diffraction.
Assume that are three crystal lattice vectors in a crystal
Similarly,

## Slide 11
Very often , the Laue conditions are expressed as
Unit vector
The three Laue conditions must be satisfied
simultaneously for diffraction to occur.
The physical meaning of the 3 Laue conditions
are illustrated below.

## Slide 12
1st Laue conditions
The path difference
between the waves
equals to
The criterion for diffraction to occur is
or
integer

## Slide 13
For 1-dimensional crystal
Cones of diffracted beams for different h

## Slide 15
Stereographic projection representation for 1-D crystals
The projection of diffracted beams for h = 0 is a great circle if the incident beam direction is perpendicular, i.e.
The projection of diffracted beams for h = 0 is a small circle if the incident beam direction is not perpendicular

## Slide 16
2nd Laue condition
integer

## Slide 17
For a two-dimensional crystal
The 1st and 2nd conditions are simultaneously satisfied only along lines of intersection of cones.

## Slide 18
Stereographic projection for 2-D crystals
The lines of intersection of cones are labeled as (h , k)

## Slide 19
3rd Laue condition
l: integer
For a single crystal and a monochromatic wavelength, it is usually no diffraction to occur

## Slide 20
(2) Laue photograph
Laue photograph is performed at “ single crystal and variable wavelength ”.
(2-1) Ewald sphere construction
or
white radiation : wavelength is continuoue;
lwl and swl: the longest and shortest wavelength in the white radiation.

## Slide 21
Two Ewald spheres of radius OA and OB form
in between two spherical surface meets the diffraction condition since the wavelength is continuous in white radiation.

## Slide 22
http://www.xtal.iqfr.csic.es/Cristalografia/archivos_06/laue1.jpg

## Slide 23
(2-2) zone axis
The planes belong to a zone
We define several planes belong to a zone [uvw], their plane normal [hi ki li] are perpendicular to the zone axis, In other words,

## Slide 24
In the Laue experiments, all the planes meet the diffraction criterion. Each plane meets the 3 Laue conditions.
for all the plane belonged to the zone [uvw].

## Slide 25
If we define
The path difference between the waves equals to

## Slide 26
(A) for the condition  < 45o
For all the planes (hikili) in the same zone [uvw]

## Slide 27
Therefore, all the diffracted beam directions Ŝ1', Ŝ2', Ŝ3', …Ŝi' are on the same cone surface.
(B) for the condition  > 45o
The same as well

## Slide 28
    9-2-2 Diffractometer method

## Slide 29
Instrumentation at MSE, NTHU
Shimatsu XRD 6000

## Slide 30
Rigaku TTR

## Slide 31
Bruker D2 phaser

## Slide 32
9-2-2-1 -2 scan

## Slide 33
If a new material is deposited on Si(100) and put on the substrate holder in the diffractometer set-up, is always parallel to the Si(100) surface normal.
Any sample
1
2

## Slide 34
Rotate the incident beam at until meets the diffraction condition at
Ewald sphere construction
1
21
Si (100) substrate
o

## Slide 35
This is equivalent to at least one crystal with
(h1k1l1) plane normal in parallel with the
Si(100) surface normal.
When the incident beam is rotated (rotating
the Ewald sphere or rotating the reciprocal
lattice), will meet the diffraction
condition at
1
22
Si (100) substrate
o
2

## Slide 36
This is equivalent to at least one crystal with
(h2k2l2) plane normal in parallel with the
Si(100) surface normal.
If only one plane of the film is observed in the diffractometer measurement, the film is epitaxial or textured on Si(100).

## Slide 37
(b) XRD spectrum of AlN deposited on Si(100)
A large number of grains with AlN(002) surface normal in parallel to Si(100) surface normal, but small amount of grains of AlN(100) and AlN(101) are also in parallel to Si(100) surface normal.

## Slide 38
9-2-2-2 X-ray rocking curve
X-ray rocking is usually used to characterize the crystal quality of an epitaxial or textured film.
At a certain diffraction condition
the incident and outgoing directions of X-ray are fixed and the sample is rotated by  scan.
Careful scan around a specific diffraction
peak!

## Slide 39
When the crystal is rotated by d, this is equivalent
to the detector being moved by the same d. (?) The FWHM of the diffracted peak truly reflects the
width of each reciprocal lattice point, i.e. the
shape effect of a crystal. (by high resolution!)

## Slide 40
2
o
2(+)
o

## Slide 41
9-2-2-3.  Scan
The  scan is used to characterize the quality of the epitaxial film around its plane normal by rotating  (0-2)


## Slide 42
Example: the crystal quality of highly oriented grains each of which is a columnar structure shown below
Each lattice point in the reciprocal lattice will be expanded into an orthorhombic volume according to the shape effect. The scan can be used to confirm the orientation of the columnar structure relative to the substrate.

## Slide 43
Shape effect
grain
(
)
Reciprocal
lattice points
2
2

## Slide 44
2

0
360

## Slide 45
9-2-4 Powder method (Debye-Scherrer Camera)
http://www.adias-uae.com/plaster.html

## Slide 46
http://www.stanford.edu/group/glam/xlab/MatSci162_172/LectureNotes/06_Geometry,%20Detectors.pdf

## Slide 47
(a) Ewald sphere construction
Reciprocal lattice of a polycrystalline
sample
B.D. Cullity
Reciprocal lattice become a series of concentric
spherical shells with as their radius
Powder can be treated as a very larger number of polycrystals with grain orientation in a random distribution

## Slide 48
Intersection of Ewald
sphere with spherical
reciprocal lattice!
forms a cone resulting from the intersection between Ewald sphere and the spherical reciprocal lattice.
The intersection between the concentric spherical shells of in radius and the Ewald sphere of radius are a series of circles (recorded as lines in films)

## Slide 49
Example
Debye-Scherrer powder pattern of Cu made with Cu K radiation

## Slide 50
1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
line | hkl | h2+k2+l2 | sin2 | sin |  (o) | sin/(Å-1) | fCu
1 2 3 4 5 6 7 8 | 111 200 220 311 222 400 331 420 | 3 4 8 11 12 16 19 20 | 0.1365 0.1820 0.364 0.500 0.546 0.728 0.865 0.910 | 0.369 0.427 0.603 0.707 0.739 0.853 0.930 0.954 | 21.7 25.3 37.1 45.0 47.6 58.5 68.4 72.6 | 0.24 0.27 0.39 0.46 0.48 0.55 0.60 0.62 | 22.1 20.9 16.8 14.8 14.2 12.5 11.5 11.1

## Slide 51
1 | 9 | 10 | 11 | 12 | 13 | 14
line | ¦F¦2 | P |  | Relative integrated intensity |  | 
 |  |  |  | Calc.(x105) Calc. Obs. |  | 
1 2 3 4 5 6 7 8 | 7810 6990 4520 3500 3230 2500 2120 1970 | 8 6 12 24 8 6 24 24 | 12.03 8.50 3.70 2.83 2.74 3.18 4.81 6.15 | 7.52 3.56 2.01 2.38 0.71 0.48 2.45 2.91 | 10.0 4.7 2.7 3.2 0.9 0.6 3.3 3.9 | Vs S s s m w s s
111
200
220
311
222
400
331
420

## Slide 52
(a) Structure factor (Cu: Fm-3m, a = 3.615 Å)
Four atoms at [000], [½ ½ 0], [½ 0 ½],
[0 ½ ½]

## Slide 53
If h, k, l are unmixed
If h, k, l are mixed
(b)
Small  is associated with small h2+k2+l2.

## Slide 54
Example: 111

## Slide 55
0 0.1 0.2 0.3 0.4
29 27.19 23.63 19.90 16.48
p = 8
(23 = 8)

## Slide 56
(c) Multiplicity P is the one counted in the
point group stereogram.
In Cubic (h  k  l)
{hkl}
{hhl}
{0kl}
{0kk}
{hhh}
{00l}
P = 48
P = 24
P = 24
P = 12
P = 8
P = 6
(3x2x23)
(3x23)
(3x2x22)
(3x22)
(23)
(3x2)
How about tetragonal?

## Slide 57
(d) Lorentz-polarization factor
(i) polarization factor
The scattered beam depends on the angle of
scattering. Thomson equation
I0: intensity of the incident beam
K: constant
: angle between the scattering direction and the direction of acceleration of the electron
r

P
e

## Slide 58
incident beam travel in direction
Random polarized beam 

## Slide 59
The intensity at point P
y component
 = yOP = /2
z component
 = zOP = /2 -2
Polarization factor

## Slide 60
(ii) Lorentz factor
(ii-1)
factor due to grain orientation or crystal rotation
The factor is counted in powder method and in rotating crystal method.
First, the integrated
intensity

## Slide 61
(a)
Crystals with reflection planes make an angle
B with the incident beam  Bragg condition
met  intensity diffracted in the direction 2B.
But, some other crystals are still diffracted in
this direction when the angle of incident
differs slightly from B!

## Slide 62
2B
Intensity
Diffraction Angle 2
Imax
Imax/2

2
Integrated
Intensity
B
2
1
2
A
B
a
2
C
D
Na
1
N
B
2
1
2
1
path difference for 11-22
= AD – CB = acos2 - acos1
= a[cos(B-) - cos (B+)]
= 2asin()sinB ~ 2a sinB.
2Na sinB =   completely
cancellation (1- N/2, 2- (N/2+1) …)
Maximum angular range of the peak

## Slide 63
(b)
the width B increases as the thickness of the crystal decreases , as shown in the figure in the next page

## Slide 64
t = mdhkl




 + 
 + 
…
…
0
1
2
m
Constructive Interference
   + 
   + .
…
Destructive interference:
extra path difference (plane 0 and plane m/2): /2

## Slide 65
 << 1s  cos ~ 1 and sin ~ .
= t
Broadening (B): FWHM
Thickness dependent (just like slits)

## Slide 66
(iii-1) :factor due to the number of crystal counted in the powder method
The number of crystal is not constant for a
particular B even through the crystal are oriented completely at random.

## Slide 68
For the hkl reflection, the range of angle near the Bragg angle, over which reflection is appreciable, is . Assuming that N is the number of crystals located in the circular band of width r.
# of grains satisfying the diffraction condition  cosB.
 more grains satisfying the diffraction condition at higher B.

## Slide 69
(iii-2) factor due to the segment factor in the Debye-Scherrer film
The film receives a greater proportion of a diffraction cone when the reflection is in the forward or backward direction than it does near

## Slide 70
The relative intensity per unit length is proportional to
i.e. proportional to
Therefore, the Lorentz factor for the powder method is
and for the rotating crystal method and the diffractometer method is

## Slide 71
(iv) Plot of polarization and Lorentz factors